Central Loose Tube Aerial Self Supported, G.652D, FRP, MDPE

Cable Design

Technical data

| Fibers of cable |  | 2~12 |
| --- | --- | --- |
| Span |  | 120m |
| Fiber Model |  | G.652D |
| Loose Tube | Material | PBT |
|  | Diameter | 2.1±0.1 mm |
|  | Thickness | 0.35±0.05 mm |
|  | NO. | 1 |
|  | Color | Natural |
| Strength Member | Material | FRP |
|  | Diameter | 2.1±0.05 mm |
|  | NO. | 2 |
| Water Blocking | Material | Water Blocking Yarn |
| Rip Cord | Material | Nylon |
|  | NO. | 1 |
| Outer Sheath | Material | MDPE |
|  | Color | Black |
| Cable Diameter |  | 7.4±0.2 mm |
| Cable Weight |  | 49±5.0 kg/km |
| Allowable Tensile Strength |  | 2000N |
| Allowable Crush Resistance |  | 2200N/100mm |
| Min. bending radius | Without Tension | 12.5×Cable-φ |
|  | Under Maximum Tension | 25.0×Cable-φ |
| Temperature range （℃） | Installation | -20~+60 |
|  | Transport &Storage | -40~+70 |
|  | Operation | -40~+70 |

Fibre Color

| No. | 1 | 2 | 3 | 4 | 5 | 6 |
| --- | --- | --- | --- | --- | --- | --- |
| Color | Green | Yellow | White | Blue | Red | Violet |
| No. | 7 | 8 | 9 | 10 | 11 | 12 |
| Color | Brown | Pink | Black | Grey | Orange | Aqua |

The properties of single mode optical fiber (ITU-T Rec. G.652.D)

| Item | Specification |
| --- | --- |
| Fiber type | Single mode |
| Fiber material | Doped silica |
| Attenuation coefficient @ 1310 nm @ 1383 nm @ 1550 nm @ 1625 nm |  0.35 dB/km  0.32 dB/km  0.21 dB/km  0.25 dB/km |
| Point discontinuity |  0.05 dB |
| Cable cut-off wavelength |  1260 nm |
| Zero-dispersion wavelength | 1300 ~ 1324 nm |
| Zero-dispersion slope |  0.092 ps/(nm2.km) |
| Chromatic dispersion @ 1288 ~ 1339 nm @ 1271 ~ 1360 nm @ 1550 nm @ 1625 nm | 3.5 ps/(nm. km) 5.3 ps/(nm. km) 18 ps/(nm. km) 22 ps/(nm. km) |
| PMDQ (Quadrature average*) | 0.2 ps/km1/2 |
| Mode field diameter @ 1310 nm | 9.2±0.4 um |
| Core / Clad concentricity error |  0.5 um |
| Cladding diameter | 125.0  0.7 um |
| Cladding non-circularity | 1.0% |
| Primary coating diameter | 245  10 um |
| Proof test level | 100 kpsi (=0.69 Gpa), 1% |
| Temperature dependence 0oC~ +70oC @ 1310 & 1550nm |  0.1 dB/km |

MECHANICAL AND THERMAL PERFORMANCES

| DESCRIPTION | VALUES | REFERENCES |
| --- | --- | --- |
| Tensile Strength | Load 2000N for 10 minutes .Variation of attenuation≤0.1dB .Fibers strain≤0.20% | IEC 60794-1-2-EIA IEC 60794-1-2-EIB IEC 60794-2-50 |
| Crush Tset | Load 2000N for 3 minutes .Variation of attenuation≤0.1dB | IEC 60794-1-2-E3 IEC 60794-2-50 |
| Inpact Test | Energy=1 J on surface of 12.5mm radius,3 times .Variation of attenuation≤0.1dB | IEC 60794-1-2-E4 IEC 60794-2-50 |
| Bending Test | Load 100N for 5 minutes Radius of curvature=10×O.D .Variation of attenuation≤0.1dB | IEC 60794-1-2-E18A Procedure no.2 |
| Kink Test | No kink with loop diameter of 10 mm | IEC 60794-1-2-E10 |
| Tinght buffer removal | Length of 0.3m in a single operation | IEC 60794-1-2-E5 IEC 60794-1-32 |
| Outer sheath removal | Load≤15N for removing sheath | IEC 60794-2-50 IEC 60793-2-50-E21 |
| Tehrmal Cycles | Range -40℃/+70℃@1550nm .Variation of attenuation≤0.1dB | IEC 60794-1-2-F1 IEC 60794-2-20 |
| UV Resistant | ±30% after aging | CEI EN 50289-4-17 Method A |

Sheath marking

The optical fiber drop cable shall have sequentially numbered length marking at intervals of approximately 1 meter. The starting number of ordering length for any coil shall begin whit zero meter. The accuracy of the measurement of lenth marking shall be held within the limits of ±1%.

- Manufacturer’s name

- Type of wire

- Year and month of manufacture

- Length marking each meter along the wire

HEADWAY  GYXFTY-××B1-××m    2024   =0001m=

×

- （b）               （c）     （d）